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	1
	Basic description:





	

	
	
Slurry:
1. Gypsum Slurry of Hemi-Hydrate and free water at an approximate ratio of 4.2: 5 (Gypsum to water) on a weight basis.

	

	2
	SPECIFICATION (Properties at 85OC):
	

	
	1. APPEARANCE: Milky-white Slurry  
2. BULK DENSITY: 
Free flowing: ~1,600 Kg/m3
Solids (Settled): 2,700 Kg/m3
Liquid (Filtrate): ~1,000 Kg/m3
3. TEMPERATURE, OC: <80-100OC
4. FLOWABILITY: Temperature dependent, higher temperature greater flowability
5. ABRASION: Low-medium (depending on temperature/settling factors)
6. ESTIMATED PARTICLE SIZE DISTRIBUTION (PSD): 

D10: 16 µm
D50: 30 µm
[bookmark: _GoBack]D90: 52 µm

7. pH: 6-7 
8. CHEMICAL COMPOSITION BY WEIGHT:
                       W/W HEMIHYDRATE: ~45 %
                       W/W FREE WATER: ~54.3 %
                       W/W SUCCINIC ACID: <0.001 %
                       W/W SODIUM: 0.003%
                       W/W CHLORIDE: 0.01%
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